| Flexible Pavement TECHNICAL GUIDE | TG 02740 |
| --- | --- |

1.	COORDINATION ISSUES:

1.1	Finish wearcoat:  on playcourts shall be in accordance with TG 02790 - Athletic and Recreational Surfaces.

2.	DESIGN ISSUES:

2.1	Standards:  If your project entails work in a street or highway right-of-way, ensure conformance with the following:

2.1.1	City streets: Ordinances and Standards of the respective County government.

2.1.2	State and/or Federal - Aid highways:   Standards of the State of Hawaii and/or the Federal Government, as applicable.  Reference latest adopted edition amendment to standards.

2.2	Aggregate Subbase: Use aggregate subbase course only if required due to soil and grading conditions.

2.3	Pavement Design:  Design and designate pavement section thickness (i.e. subbbase, base course and asphaltic concrete pavement) on drawings to suit wheel load and traffic conditions.

2.4	Tack Coat: Do not apply a tack coat to sides of concrete curb and sidewalks.

3.	DRAWING NOTES:

3.1	Construction Tolerances for Slopes on Accessible Routes:

3.1.1	Include the following drawing note:

“Design slopes for accessible parking spaces, access aisles and accessible routes are less the maximum slopes allowed by the applicable Accessibility regulations.  Slopes installed in excess of the regulation maximum will be considered defective work, and shall be corrected.”

3.1.2	Include on the same drawing a list of the Accessibility regulation maximum slopes for accessible parking spaces, access aisles, and accessible routes.

4.	STANDARD DRAWINGS:

4.1	Standard Details:  If any details from the counties’ STANDARD DETAILS FOR PUBLIC WORKS CONSTRUCTION, dated September, 1984, are to be followed, note the exact detail on drawing.

5.	SPECIFICATION NOTES:

5.1	Specification Paragraphs:  As of 03/2003, a complete Guide Specification for Asphaltic Concrete Pavement is no longer being maintained by DAGS.  Utilize the following specification paragraphs and information as appropriate in the development of the Project Specifications.

5.2	Availability of Navy Tennis Court Mix:  this mix is not available on all Islands.

5.3	Criteria for use of Prime Coat:  The criteria for slope and pavement thickness noted is in accordance with guidance provided by the City & County of Honolulu. However, delete the prime coat if project conditions warrant it (For example, even if the criteria noted requires the use of a Prime Coat, delete its use where adjacent classrooms will be occupied during its application. In such cases, use the Tack Coat in its place.)

6.	GUIDE SPECIFICATION:

6.1	Materials (Part 2)

6.1.1	Materials for roads and parking areas, playcourts, walkways, and other foot traffic areas shall be in accordance with the appropriate Sections of the State of Hawaii Department of Transportation HAWAII STANDARD SPECIFICATIONS FOR ROAD, BRIDGE AND PUBLIC WORKS CONSTRUCTION, dated 1994; and the counties’ STANDARD DETAILS FOR PUBLIC WORKS, dated September 1984, as revised, except as amended in the drawings or specifications. Paragraphs concerning Measurements and Payments in the sections are not applicable. Where recycled glass is available at a cost no greater than that of the equivalent aggregate, the aggregate base course and subbase course shall contain recycled glass as specified in Section 717 of the DOT Standard Specifications.

6.2	Mixes (Part 2)

6.2.1	Roads and Parking Areas:  Use Mix No. IV and No. V for roads and parking areas respectively. Use Mix No. V for resurfacing of existing roads and parking areas. Use Mix No. III for heavy traffic / delivery areas.

6.2.2	Playcourts, Walkways, and other Foot Traffic Areas: Use Mix No. V, which is coarser that the Navy Tennis Court Mix and requires a Finish Wearcoat.

6.3	Prime Coat: (Part 2)

6.3.1	Provide a prime coat over newly constructed base course where the longitudinal grade of the pavement is  8% or more, or where the asphaltic concrete pavement thickness is less than 4 inches.

6.3.2	Where a prime coat is provided, control runoff and protect adjacent work, property, utilities, waterways, and other areas against damage.

6.4	Tack Coat: (Part 2)

6.4.1	Provide a Tack Coat in lieu of a Prime Coat in situations where the impact of its objectionable odor, potential health hazards (especially with children) or the potential for the contamination of waterways in the event of runoff are likely.

END OF SECTION 02740