| Fences and Gates TECHNICAL GUIDE | TG 02820 |
| --- | --- |

1.	COORDINATION ISSUES: (Not Used)

2.	DESIGN ISSUES: For local areas subject to severe salt exposure (such as The North Shore of Oahu), modify these guides and specifications accordingly.  Greater corrosion protection is required.

3.	DRAWING NOTES:

3.1	Indicate on drawings or details:

3.1.1	Line post spacing.

3.1.2	Required clearance of fabric from ground.

4.	STANDARD DRAWINGS:

4.1	The State Division of Public Works, Design Branch's "Chain Link Fence Details" sheet shall be used for all DAGS projects. Check User Agency Requirements.

5.	SPECIFICATION NOTES:

5.1	Materials:

5.1.1	Chain Link Fence Fabric: Hot-dip galvanized and conforms to ASTM A392, Class 1.   Fabric may be standard Chain Link or Flat Link by Von Cypher Fence Products.

5.1.2	Aluminum clad fabric conforming to ASTM A491 shall be an acceptable alternate to the hot-dipped galvanized fabric provided it is of the same gauge as the latter.

5.1.3	Change standard mesh size to 1-3/4" for tennis courts.

5.1.4	Composition and Finish of Metal Parts: All metal parts and fittings, including tracks, gate hardware, frames and fasteners shall be of steel, malleable iron or wrought iron and shall be galvanized by the hot-dip process, after fabrication, in conformance with ASTM A153.

5.1.5	Fence Gate Hardware: Specify padlock in the fences and gates section only if project specification does not include a hardware section.

5.1.5.1	Padlock shall be 5-pin cylinder type with brass case and a 5/16" dia. hardened steel shackle.  Padlocks shall be keyed differently but masterkeyed to the fence system.  Two masterkeys shall be provided.

5.1.5.2	Check with user to master key padlock into complex/building.

5.1.5.3	Specify requirement for chain if needed.

5.1.6	Posts, Rails and Braces: Use standard weight, hot-dipped galvanized, welded and seamless steel pipes conforming to ASTM A120.  As an alternate, hot-dipped galvanized pipes with chromate conversion and polyurethane coatings ("Tuf 40" by American Tube Co., Inc. or approved equal) are acceptable provided posts shall be sized in accordance with and have the minimum properties shown in the table below.  Additionally, Tuf 40 type pipes shall not be used where welded pipe frames are called for.

Dimensions and Weights of Tuf 40 Steel Pipe Posts

Post Type/Fence Ht.	Nom.Dim. 	O.D.	 I.D.	Weight

( */ft.)      	(in.)   	 (in.)  	(in.) (lbs/ft)

Rails only        	1-5/8   	1.660	1.440	1.82

L/4          		1-7/8	1.900	1.660	2.28

L/6-8; T/4        		2-3/8	2.375	2.115	3.12

L/10,12; T/6-8 		2-7/8	2.875	2.555	4.64

*L - Line posts; T - Terminal posts

5.2	Installation and Workmanship

5.2.1	Make sure to address section to meet standards gates and hardware to provide intended freedom of operation, posts shall be plumb and in line, welding shall be done in accordance with latest AWS standards. Do not allow splicing of posts, rails or braces.

5.2.2	Post and Rail Installation:

5.2.2.1	Provide a corner post where fence direction change exceeds 30 degrees or more.

5.2.2.2	End, corner, and gate posts for fences with 5-foot and wider fabric shall be braced to the nearest line post with horizontal braces and tension rods.  The horizontal braces shall be spaced midway between top rail and ground and securely fastened to posts.

5.2.2.3	Where fencing is placed along a curve with radius of 50 feet, or less, horizontal braces (and tension rods) shall be installed between all posts in like manner. Pull posts, at maximum intervals of 300 feet, shall be braced and trusses in both directions as specified above.

5.2.2.4	Couplings for the top rails: Install at intervals of 24 feet maximum.

5.2.3	Chain Link Fabric Installation:

5.2.3.1	Fasten fabric on the side of the posts.

5.2.3.2	Mount fabric on the posts so that the bottom of the fabric will be no more above the finished grade than indicated on the plans.

5.2.3.3	Excavate high points of the ground if necessary to allow fabric to maintain the indicated clearance.

6.	GUIDE SPECIFICATION: (Not Used)

END OF SECTION 02820