| Plant Precast Structural Concrete TECHNICAL GUIDE | TG 03410 |
| --- | --- |

1.	COORDINATION ISSUES: (Not Used)

2.	DESIGN ISSUES:

2.1	Buckling of continuous longitudinal weld plates:

2.1.1	Problem:  Because of relatively large amounts of creep in prestressed concrete members, we have had a problem with the buckling of continuous weld plates anchored longitudinally in beams to receive welded studs for supporting operable partitions. The buckling is especially severe where the operable partition was not installed initially because of incremental construction.

2.1.2	Solution:  To preclude this problem, the following are suggested as alternatives to the above and shall be considered for use when the design requires a similar application:

2.1.2.1	Use discontinuous or intermittent weld plates.  In this instance, be sure to specify or call out that weld plate locations shall be coordinated with the supplier of whatever is to be supported on them.

2.1.2.2	Use continuous weld plate attached so there is some "give" in the longitudinal direction.  See Detail A/TG03410

2.1.2.3	Use removable cylindrical plastic inserts which can be replaced with expansion anchors when the partition support plate is installed later.  See Detail B/TG03410.

3.	DRAWING NOTES: (Not Used)

4.	STANDARD DRAWINGS:   See Attached Drawings.

Detail A:	Weld Plate at Prestressed Concrete (installed during construction.)

Detail B:	Weld Plate at Prestressed Concrete (installed post-construction.)

5.	SPECIFICATION NOTES: (Not Used)

6.	GUIDE SPECIFICATION:  (Not Used)

END OF SECTION 0341