| Membrane Waterproofing TECHNICAL GUIDE | TG 07110 |
| --- | --- |

1.	COORDINATION ISSUES:

1.1	Vertical waterproofing: Coordinate the detailing of the waterproofing drainage/ protection board with a foundation drainage system or other engineered means of reducing the hydrostatic pressure from below grade saturated soil.

1.2	Refer to Division 9 sections for waterproof membrane for use under thin-set ceramic and quarry tile.

1.3	For horizontal between slab applications (decks over habitable spaces), consultant shall obtain Quality Control Branch’s approval of design, details and materials specified.

2.	DESIGN ISSUES: (Not Used)

2.1	Vertical waterproofing: Most membranes and protection boards cannot be exposed to ultraviolet light, landscaping or traffic. Detail a protected termination condition suitable for the waterproofing technology used and acceptable to the waterproofing membrane manufacturer.

2.2	Be advised that the membranes noted in this Technical Guide are intended for use in below-grade and between slab applications.  They are not intended for use under thin-set ceramic or quarry tile floor installations.

3.	DRAWING NOTES:

3.1	Indicate on drawings or details:

3.1.1	For toilets, showers and other similar areas, the membrane shall be extended 4" up adjacent vertical surfaces or 4 inches above the finished floor level, whichever is higher.

4.	STANDARD DRAWINGS:  (Not Used)

5.	SPECIFICATION NOTES:

5.1	Submittals:

5.1.1	Request installing contractor’s current applicator license.

5.1.2	Request a signed certificate from the membrane waterproofing manufacturer stating that the Contractor is an approved applicator.

5.1.3	Request manufacturer's material specifications, application instructions and Material Safety Data Sheets for the proposed membrane waterproofing system and materials.

5.1.4	Request manufacturer’s proposed guarantee form.

5.2	Warranty

5.2.1	The warranty provisions and number of years for the warranty required by this article shall take precedence over standard provisions in the General Conditions.

5.2.2	Require a three year warranty covering the waterproofing installation and to repair any leaks which develop during that period which are not due to improper use or willful damage.

5.3	Cautions and Warnings: Include the following caution:

5.3.1	“Vapors from bonding adhesives, lap cements, membrane material products, or other accessory materials may be harmful if inhaled or placed in contact with the skin. Vapors may also be flammable.  Consult container labels and Material Safety Data Sheets for specific information and employ safety precautions needed for the products being used.”

5.4	Manufacturers

5.4.1	The following products, or their predecessor products, have been used successfully on DAGS projects. Products of other manufacturers may be specified subject to the judgment of the design professional and recognized third party product testing and the appropriateness of the product to the particular project conditions.

5.4.1.1 Carlisle Coatings and Waterproofing:				CCW-701 (formerly QSC-701)

5.4.1.2	Protecto Wrap Co.:										Jiffy Seal 140/60

5.4.1.3	Polygard Products, Inc.:									Polygard 650

5.4.1.4	Royston Laboratories:									104-AHT

5.4.1.5	WR Grace & Co.:											Bituthene 3000

5.5	Horizontal waterproofing:   Include the following minimum testing requirements:

5.5.1	Horizontal membranes placed between slabs located above usable space shall be water tested for at least 24 hours under a head equal to the thickness of the floor finish to be placed atop the depressed floor slab plus 1 inch as measured from the slab high point. Any leaks detected shall be sealed and the membrane similarly re-tested until it is watertight. A detectable reduction in water level detectable after 24 hours and not attributable to normal evaporation shall also be considered evidence of leakage.

5.5.2	Notification of Contracting Officer 24 hours in advance before membrane is tested.

5.5.3	Fluid-applied membranes shall be subject to compliance testing by Engineer to ensure proper thickness of application.

5.6	Provision of Thinset Waterproofing Membrane:

5.6.1	General: Where a thin-set installation is required, the consultant shall modify the specification section to include the appropriate types of membranes.

5.6.2	Cautions:  Thin liquid-applied membranes whose performance is greatly dependent upon the workmanship of the applicator and tile installer shall not be specified. The thickness of the membrane is difficult to control and the membrane can easily be abraded or punctured during tile installation.

5.6.3	Renovations:  Where existing above-grade toilet/shower facilities are being renovated (e.g. existing floors are being repaired/replaced, partition floor anchors or other devices penetrating the membrane are being removed, etc.) the scope of work shall include the repair or replacement of the existing waterproofing membrane as necessary to provide a watertight assembly.

6.	GUIDE SPECIFICATION: (Not Used)

END OF SECTION 07110